## Slide 1
PPPL Experiment Seminar
Wednesday, February 21, 2001
Li capillary porous system on T-11M
Gettering of Deuterium and He
Deuterium retention in Li limiter

## Slide 2
Liquid metal activity in tokamak research.
“Red Star”-TRINITI collaboration in Russian Federation.

## Slide 3
Gallium droplet limiter
(experiments were done on T-3M tokamak in Shatura, in1984-85.
Gallium film (gravity driven) limiter
(experiments were done on T-3M in Shatura, in 1986-88)

## Slide 4
Scheme of “Radiative Li Divertor” with porous capillary divertor plates
for ITER-like tokamaks

## Slide 5
Photo-picture of the surface of the Li filled capillary mesh system with 100 micron thick Molybdenum wires.

## Slide 6
Power of total Li radiation as a function of the electron plasma temperature.
Different curves correspond to different products of the plasma density and the Li life time in the plasma.

## Slide 7
Positioning of the Li capillary mesh limiter and a conventional carbon limiter at T-11M.
Any of the limiters can be moved out of plasma touch.

## Slide 8
Rail limiter with the Li capillary porous system at the top of moving stick.

## Slide 9
Two designs of the Li capillary rail limiter.
Variant I ejected Li droplets during the plasma disruptions.
Improved, Variant II can withstand the disruptions with no droplet expulsion.

## Slide 10
Traces of droplets at the port walls for Var. I (limiter was removed while picturing).
Var.I. Enhanced view on back side of the vacuum chamber and on the plasma facing surface of the wall.
Variant II of the Li limiter generated no droplets on the walls.

## Slide 11
Description of T-11M AXUV diagnostics system.
Similar system is used on CDX-U.

## Slide 12
Sensitivity characteristics of the silicon AXUV detectors used on T-11M.

## Slide 13
Energy deposition on the Li limiter (top-left picture) during a typical discharge on T-11M (reported at the ISFNT meeting, Madrid, Spain, August, 2000)

## Slide 14
Temporary behavior of the Li radiation during the T-11M discharge for different initial temperatures of the CPS limiter.

## Slide 15
He discharges on T-11M with the hot Li limiter demonstrate reduction in the plasma density with the number of discharges.
Explained by the gettering effect of the Li coating of the side walls.

## Slide 16
He discharge with limiters removed and walls heavily coated by Li.
Wave form of the plasma current.
Waveform of the electron plasma density showing a large gettering effect of the walls.
Waveform of Shafranov shift.
Waveform of the SX signal showing suppression of runaway electrons.

## Slide 17
He pressure reduction during the discharge and recovery after the discharge for different initial pressure in the discharge chamber. Speed of the vacuum pumping system was reduced.
Room temperature of the walls. Wall heating eliminates the effect.

## Slide 18
Deuterium discharges: Plasma current waveform.
Electron density for normal gas puffing with Li and C limiter, and for maximum gas puffing with Li coated walls.
Density rump down due to wall gettering effect after one gas puffing pulse.

## Slide 19
Density behavior in the maximum gas puffing deuterium discharge after shutting down the gas puffing.
D_alpha behavior at the gas puffing port.

## Slide 20
High Li limiter temperature discharge with the H2 puffing. Waveforms of the plasma current, emission at the puffing port, resistive voltage, H_alpha emission at the Li limiter, “Spitzer Te”, visible Li limiter light, SXR, light from the C-limiter zone, plasma density, and the total radiation power.
While the hydrogen content is dropping, the content of Li in plasma is increasing.

## Slide 21
Power (relative to the ohmic heating) released at the Li limiter (y-axis) drops with an increase of the initial temperature (x-axis) of the limiter, thus, suggesting a “self-protection” by the Li irradiation.

## Slide 22
Release of deuterium (total amount of about 4 single discharge contents). The Li limiter was gradually heated for about 30 min after an experimental campaign.

## Slide 23
Summary:
Free surface metal is vulnerable to disruptions.
CPS can withstand the disruptions.
Li covered walls getter both He and D.
Heating of CPS leads to the hydrogen release.