## Slide 1: F L I R E Flowing Liquid-Surface Illinois Retention Experiment Critical Design Considerations
Mark Boaz, David N. Ruzic, Ning Li,
Jeff Norman and Jean-Paul Allain
Department of Nuclear, Plasma, and Radiological Engineering
University of Illinois
at Urbana Champaign
October 25, 2000 APS DPP Meeting

## Slide 2: Outline
Motivation
FLIRE Concept
Experiment to Address Critical Concern
Results
Conclusion
Acknowledgements

## Slide 3: Motivation
Flowing Liquid Metal Walls
  High heat flux capability
  Disruption resistant
  Low Z possible
  May have new plasma operating regimes
Can helium be removed ?
What is the retention of He in liquid metals?

## Slide 4: Proposed Experiment
Flow Li down a ramp into a second vacuum system inside the large vacuum system
Have Li flow provide vacuum isolation
Aim He ion beam at flowing Li
Look for He in inner chamber with a He leak detector

## Slide 9: Detectability Limits
He leak detectors can see 2.7 x 109 s-1
Ion beam at 1 mA has 1.6 x 1016 s-1
(seven-orders-of-magnitude !)
Flow velocity = 1 m/s
Fusion system will have same time in chamber, 0.01 sec.
If 1 ppm is seen, (six-orders-of-magnitude) minimum observable retention time constant = 25 sec.

## Slide 10: Critical Questions
Will surface layer with the implanted ions smoothly flow into the inner vacuum chamber or will the liquid metal pool at the opening?
If it does not pool, will a vacuum seal be maintained?
Is having two ramps sufficient to ensure this?

## Slide 11: Prototype Design
Key is to have flow maintain contact with ramps.
Equation of motion for free flow:
y(x) = x - bx2
Measure flow speed, find “b”, cut plywood.
Length of ramp determined by co-joining angle. Experiment, choose 25 degrees.

## Slide 12
slotted holes in plywood allowed for adjustment of exit size

## Slide 13
gap from reservoir controlled by teflon insert

## Slide 14
Exit
width
is
3 mm

## Slide 15
Assembled FLIRE prototype

## Slide 16
Note brightness of exit when open

## Slide 17
5 mm gap from reservoirs is too big !

## Slide 18
4 mm gap still pools, but then settles down nicely

## Slide 19
3 mm gap is just right

## Slide 20
2 mm gap is okay, but some Cu is showing

## Slide 21
3 mm gap again, different view

## Slide 22: Conclusion
Through careful design, uniform “folding” flow can be achieved.
FLIRE experiment could determine critical parameters for the ALPS/ APEX programs

## Slide 23: Acknowledgements
DOE ALPS program
Undergraduate Research Assistants
  Hussain Nomanbhai
  Shadi Beidas